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MANUFACTURES OF INDUSTRIAL FILTER BAGS



Product Data Sheet


	Construction
	Needle Felt

	Micron Rating
	100 Micron

	Composition
	Polyester

	Weight
	300 ~ 390 g/m2

	Air Permeability
	137 ~ 240 cc/cm2/sec( 65-115 m3/m2/min)

	Tensile Strength
	25MD, 30CD KG/5cm

	Elongation
	140MD, 140CD %

	Bursting Strength
	20 kg/cm2

	Thickness
	2.55 ~ 2.85 mm

	Finish
	Non

	Operating Temp
	130(C

	Max Temp
	150(C


Characteristics.

Ideal for the filtration of particles from liquid in mild acid and alkaline environments.
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Technical details are only of an advisory nature to demonstrate the application of our products and are subject to tolerance

